Type equation here. MULTI-AXIAL LOADING: Generalised Hooke’s Law So far, we have been discussing uni-axial loading. Now, consider an element of the material is subjected to axial normal stresses in three mutually perpendicular directions. Let the side of the cube be a. The normal stresses will change the dimensions of the cube. If the material is stresses within the linear elastic range, we can apply the principle of superposition. That is, the effect of each stress is considered separately and total deformation is the algebraic sum of the individual deformations.. Only normal stresses will cause a change is dimension (or change in volume), shear stress will not. Shear stress will cause only a change in shape. The strains produced by each normal stress in three mutually perpendicular directions are given in the table below. Strain in the x-direction; Strain in the y-direction; Strain in the z-direction. Tensile stress in the x-direction, σxx; σxxE (linear strain); -νσxxE (lateral strain); -νσxxE (lateral strain). Tensile stress in the y-direction, σyy; -νσyyE (lateral strain); σyyE (linear strain); -νσyyE (lateral strain). Tensile stress in the z-direction, σzz; -νσzzE (lateral strain); -νσzzE (lateral strain); σzzE (linear strain). The net normal strain in the x-direction, εxx=σxxE-νσyyE-νσzzE The net normal strain in the y-direction, εyy=σyyE-νσxxE-νσzzE The net normal strain in the x-direction, εzz=σzzE-νσxxE-νσyyE The shear strains εxy=γxy2=τxy2G=τxy2E2(1+ν)=τxy(1+ν)E ≪≫ εyz=τyz(1+ν)E ≪≫ εzx=τzx(1+ν)E This is known as generalised Hooke’s Law for multi-axial loading. εxz εyz εxy It is left as an exercise to the students to express the stresses in terms of the strain values as shown below. σxx=νE(1+ν)(1-2ν)εxx+εyy+εzz+E1+νεxx=λe+2Gεxx εxz εyz εxy. Due to the normal strains in the three mutually perpendicular directions, the dimensions of the cube(a,a,a) will change to (a+aεxx, a+aεyy,a+aεzz). The initial volume of the cube, V=a3 The final volume of the cube, V'=a+aεxx a+aεyya+aεzz=a3(1+εxx)(1+εyy)(1+εzz) =a31+εxx+εyy+εzz+εxxεyy+εyyεzz+εxxεzz+εxxεyyεzz Since the strain values are very small, their products are still smaller and hence they can be neglected. V'=a31+εxx+εyy+εzz The change in volume, ΔV=V'-V=a3εxx+εyy+εzz The volumetric strain (Dilatation, e)=Change in volumeOriginal volumne=ΔVV=εxx+εyy+εzz e=σxxE-νσyyE-νσzzE+σyyE-νσxxE-νσzzE+σzzE-νσxxE-νσyyE e=σxx+σyy+σzzE-2νEσxx+σyy+σzz=σxx+σyy+σzz1-2νE If σxx=σyy=σzz=σ (Spherical stress or Hydrostatic stress) e=3σ1-2νE σe=E3(1-2ν) The ratio of spherical stress to volumetric strain(dilatation) is known as Bulk Modulus (K) K=E3(1-2ν) A positive σ (tensile stress) will produce a positive dilatation (increase in volume) only if 1-2ν>0 ≪≫ ν<12 For any engineering material, the Poisson’s ratio varies between 0 and 0.5. Example 1 The steel block shown is subjected to a uniform pressure on all its faces. Knowing that the change in length of edge AB is -3.05×10-3 cm, determine (a) the change in length of the other two edges, (b) the pressure p applied to the faces of the block. (c) the change in volume of the block. Assume E=200 GPa and ν=0.29; 7.5 cm 5 cm 10cm. Let p be the pressure (compressive stress) acting on all the sides. εxx=σxxE-νσyyE-νσzzE=-pE+νpE+νpE=-pE(1-2ν) εyy=σyyE-νσxxE-νσzzE=-pE+νpE+νpE=-pE(1-2ν) εzz=σzzE-νσxxE-νσyyE=-pE+νpE+νpE=-pE(1-2ν) εxx=δABLAB=-3.05×10-3 cm10 cm=-0.305×10-3 ∴ -0.305×10-3=-pE1-2ν=-p200×1091-2×0.29 ≪≫ p=145.2×106 Pa εyy=εzz=-pE1-2ν=-0.305×10-3 δBC=LBC×εyy=-1.525×10-3 cm δBD=LBD×εzz=-2.2875×10-3 cm The bulk modulus, K=E3(1-2ν)=200×1093(1-2×0.29)=158.7×109 Pa K=hydrostatic stressdilatation=-145.2×106e ≪≫ e=-9.1476×10-4 V=10 cm×7.5 cm×5 cm=375 cm3 ΔVV=-9.1476×10-4 ≪≫ ΔV=-0.3430 cm3 Example 2 A circle of diameter d=225 mm is scribed on an unstressed aluminium plate of thickness t=20 mm. Forces acting in the plane of the plate later cause normal stress σxx=83 MPa and σzz=138 MPa. For E=70 GPa and ν=0.33, determine the change in (a) the diameter AB, and CD, (b) the thickness of the plate, (d) the volume of the plate.; 380mm 380mm. The original volume of the plate, V=0.38m×0.38m×0.02m=2.888×10-3 m3 Strain in the x-direction; Strain in the y-direction; Strain in the z-direction. Stress along x-axis σxx=83 MPa; σxxE=83×10670×109=1.186×10-3 (linear strain); -νσxxE=-0.344×10-3 (lateral strain); -νσxxE=-0.344×10-3 (lateral strain). Stress along x-axis σxx=138 MPa; -νσzzE=-0.651×10-3 (lateral strain); -νσzzE=-0.651×10-3 (lateral strain); σzzE=138×10670×109=1.97×10-3 (linear strain). εxx=0.535×10-3; εyy=-0.995×10-3; εzz=1.626×10-3. Change in the diameter AB, δAB=εxx×AB=0.535×10-3×225mm=+0.1204 mm Change in the diameter CD, δCD=εzz×CD=1.626×10-3×225mm=+0.3659 mm Change in the thickness, δt=εyy×t=-0.995×10-3×20mm=-0.0199 mm Final length of the plate, Lx=3801+0.535×10-3=380.2033 mm Final breadth of the plate, Lz=3801+1.626×10-3=380.6179 mm Final thickness of the plate, Ly=20-0.0199=19.9801 mm New volume of the plate, V'=380.2033 mm×380.6179 mm×19.9801 mm=2.891×10-3 m3 #Exercise 1 An aluminium plate E=74 GPa,ν=0.33is subjected to a centric axial load that causes a normal stress σ. Knowing that, before loading, a line of slope 2:1 is sribed on the plate, determine the slope of the line when σ=125 MPa.. #Exercise 2 The block shown is made of a magnesium alloy E=45 GPa,ν=0.35. Knowing that σx=-180 MPa, determine (a) the magnitude of σy for which the change in the height of the block will be zero, (b) the corresponding change in the area of the face ABCD, (c) the change in volume of the block.. Reference: - Mechanics of Materials, 2/e, J. M. Gere & S. P.Timoshenko, CBS Publishers. - Mechanics of Materials, 6/e, F.P. Beer & E. R. Johnston, McGraw Hill - Engineering Mechanics of Solids, 2/e, E. P. Popov, Pearson Education Asia. - Mechanics of Materials, 9/e, R. C. Hibbeler, Prentice Hall.