Gas Tungsten Arc welding

Tungsten inert gas welding process also called as gas tungsten arc welding is named so because it uses a) electrode primarily made of tungsten and b) inert gas for shielding the weld pool to prevent its contamination from atmospheric gases especially when joining high strength reactive metals and alloys such as stainless steel, aluminium and magnesium alloys, wherever high quality weld joints need to be developed for critical applications like nuclear reactors, aircraft etc. Invention of this process in middle of twentieth century gave a big boost to fabricators of these reactive metals as none of the processes (SMAW and Gas welding) available at that time were able to weld them successfully primarily due to two limitations a) contamination of weld from atmospheric gases and b) poor control over the heat input required for melting (Fig. 14.1). Moreover, welding of aluminium and its alloys with shielded metal arc welding process can be realized using halide flux coated electrodes by overcoming the problems associated with Al2O3, however, halides are very corrosive and therefore welding of aluminium is preferable carried out using inert shielding environment with the lerp of processes like GTAW and GMAW. Despite of so many developments in the field of welding, TIG process is invariably recommended for joining of thin aluminium sheets of thickness less than 1mm.

14.2 TIG welding system

There are four basic components (Fig. 14.2) of TIG welding system namely a) DC/AC power source to deliver the welding current as per needs, b) welding torch (air/water cooled) with tungsten electrode and gas nozzle, c) inert shielding gas (He, Ar or their mixture) for protecting the molten weld pool contamination from atmospheric gases and d) controls for moving the welding torch as per mode of operation (manual, semi-automatic and automatic). This process uses the heat generated by an electric arc between the non-consumable tungsten electrode and work piece (mostly reactive metals like stainless steel, Al, Mg etc.) for melting of faying surfaces and inert gas is used for shielding the arc zone and weld pool from the atmospheric gases.

TIG welding with DCEP is preferred for welding of reactive metals like aluminum to take advantage of cleaning action due to development of mobile cathode spots in work piece side during welding which loosens the tenacious alumina oxide layer. This helps to clean the weld pool. DCEN polarity is used for welding of metal such as carbon steel that don’t require much cleaning.

14.2.3 Filler wire

Filler metal is generally not used for welding thin sheet by TIGW. Welding of thick steel plates by TIG welding to produce high quality welds for critical applications such as joining of nuclear and aero-space components, requires addition of filler metal to fill the groove. The filler wire can be fed manually or using some wire feed mechanism.

14.2.4 Shielding gas

Helium, Argon and their mixtures are commonly used as inert shielding gas for protecting the weld pool depending upon the metal to be welded, criticality of application and economics. Helium or hydrogen is sometimes added (1-2%) in argon for specific purposes such as increasing the arc voltage and arc stability which in turn helps to increase the heat of arc. The selection of inert gases to be used as shielding gas in GTAW and GMAW process depends upon the type of metal to be welded and criticality of their applications. Carbon dioxide is not used with GTAW process, at high temperature in arc environment, the thermal decomposition of the carbon dioxide produces CO and O2. Generation of these gases adversely affect the quality and soundness of the weld joint and reduces the life of tungsten electrode.

Inert Gases

Argon and helium are the mostly commonly used shielding gases for developing high quality weld joints of reactive and ferrous metals. Small amount of hydrogen or helium is often added in argon to increase the penetration capability and welding speed.

He vs Argon as shielding gas

A. Heat of welding arc

The ionization potential of He (25eV) is higher than Ar (16eV). Therefore, application of He as shielding gas results in higher arc voltage and hence different VI arc characteristics of arc than when argon is used as shielding gas. In general, arc voltage generated by helium for a given arc length during welding is found higher than argon. This results in hotter helium arc than argon arc. Hence, helium is preferred for the welding of thick plates at high speed especially metal systems having high thermal conductivity and high melting point.

B. Arc efficiency

Helium offers higher thermal conductivity than argon. Hence, He effectively transfers the heat from arc to the base metal which in turn helps in increasing the welding speed and arc efficiency.

C. Arc stability

He is found to offer more problems related with arc stability and arc initiation than Ar as a shielding gas. This behaviour is primarily due to higher ionization potential of He than Ar. High ionization potential of helium means it will result in presence of fewer charged particles between electrode and work piece required for initiation and maintenance of welding arc.

D. Flow rate of shielding gas

Argon (density 1.783g/l) is about 1.33 and 10 times heavier than the air and the helium respectively. This difference in density of air with shielding gases determines the flow rate of particular shielding gas required to form a blanket over the weld pool and arc zone to provide protection against the environmental attack. Helium being lighter than air tends to rise up immediately in turbulent manner away from the weld pool after coming out of the nozzle. Therefore, for effective shielding of the arc zone, flow rate of helium (12-22 l/min) must be 2-3 times higher than the argon

F. Advantages of Ar over He as Shielding Gas

For general, purpose quality weld, argon offers many advantages over helium a) easy arc initiation, b) cost effective and good availability c) good cleaning action with (AC/DCEP in aluminium and magnesium welding) and d) shallow penetration required for thin sheet welding of aluminium and magnesium alloys