Diffusion Welding

- A solid-state welding process that produces coalescence of the faying surfaces by the application of pressure at elevated temperature.

- The process does not involve macroscopic deformation, or relative motion of the workpieces.

- A solid filler metal may or may not be inserted between the faying surfaces.

- 1st stage

  - deformation forming interfacial boundary.

- 2nd stage

  - Grain boundary migration and pore elimination.

- 3rd stage

  - Volume diffusion and pore elimination.

Once clamped, pressure and heat are applied to the components, usually for many hours. The surfaces are heated either in a furnace, or via electrical resistance. Pressure can be applied using a hydraulic press at temperature; this method allows for exact measurements of load on the parts. In cases where the parts must have no temperature gradient, differential thermal expansion can be used to apply load. By fixturing parts using a low-expansion metal (i.e. Molybdenum) the parts will supply their own load by expanding more than the fixture metal at temperature. Alternative methods for applying pressure include the use of dead weights, differential gas pressure between the two surfaces, and high-pressure autoclaves. Diffusion bonding must be done in a vacuum or inert gas environment when using metals that have strong oxide layers (i.e. copper). Surface treatment including polishing, etching, and cleaning as well as diffusion pressure and temperature are important factors regarding to process of diffusion bounding.[4][5][6]

At the microscopic level, diffusion bonding occurs in three simplified stages:

Before the surfaces completely contact, asperities (very small surface defects) on the two surfaces contact and plastically deform. As these asperities deform, they interlink, forming interfaces between the two surfaces.

Elevated temperature and pressure causes accelerated creep in the materials; grain boundaries and raw material migrate and gaps between the two surfaces are reduced to isolated pores.

Material begins to diffuse across the boundary of the abutting surfaces, blending this material boundary and creating a bond.

- Application in titanium welding for  aero-space vehicles.

- Diffusion welding of nickel alloys include Inconel 600, wrought Udimet 700, and Rene 41.

- Space Shuttle designed to have 28 Diffusion Welding Components

- Dissimilar metal diffusion welding applications include Cu to Ti, Cu to Al, and Cu to Cb-1%Zr.   Brittle intermetallic compound formation  must be controlled in these applications.

Advantages

- This solid state process avoids pitfalls of fusion welding

- Dissimilar materials welds are possible

- Properties and microstructures remain similar to those of base metals

- Multiple welds can be made in one setup at the same time

- Produces a product finished to size and causes minimal deformation

- Presents less shrinkage and stresses compared to other welding processes

- Highly automated process does not need skillful workforce

Limitations

- Costly equipment especially for large weldments

- Costly preparation with smooth surface finish and exceptional cleanliness

- Protective atmosphere or vacuum required

- Long time to completion

- Not suited to high production rates

- Difference in thermal expansion of members may need special attention

- Limited nondestructive inspection methods available